## Slide 1: 6 Rubber Elasticity 橡胶弹性
Polymer Physics高分子物理

## Slide 2: 6.1 Rubber and Rubber Elasticity
Chapter 6

## Slide 3
10
9
8
7
6
5
4
3
III
I
II
IV
log G, Pa
Temperature

## Slide 4: Types of rubbe
natural rubber
synthetic rubber
Goodyear Tire
Hevea Brasiliensis 橡胶树
polybutadiene
Polyisobutene (Breathable)
Neoprene rubber (oil resistant)
Notes: 橡胶分为两类：天然橡胶和合成橡胶
聚异戊二烯 PIP Polyisoprene Natural Rubber 天然橡胶
Synthesize rubber——聚丁二烯 PB Polybutadiene(SBS中的B）；高不透气性 聚异丁烯 PIB Polyisobutylene； 耐油Polychloroprene 氯丁橡胶
Rubber is also called elastomer弹性体. It is defined as a cross-linked amorphous polymer above its glass transition temperature.
关于橡胶，查里·古德意（1800-1860）认为：“树胶的最明显的特性：跟其它所有物质最大的不同是有明显的弹性，它能伸长至自身长度的八倍，而不破裂，而后恢复至原来的形状，这可能是其它一些惰性物质所没有的

## Slide 5: Christopher Columbus 哥伦布 (1451-1506)
海地的印地安人土著人用一种类似牛奶的白色乳液放在木制的模子中，用烟熏的方法，蒸发掉水份来固化制成球做游戏。

## Slide 6: Goodyear Tire
Michelin Tire
Dunlop Tire
Hancock Tire

## Slide 7: The definition of rubber
施加外力时发生大的形变、外力除去后可以恢复的弹性材料称为橡胶;美国材料协会标准(ASTM-American Society for Testing and Materials)规定:20-70摄氏度下,1min可拉伸2倍的试样,当外力除去后1min内至少回缩到原长的1.5倍以下或者在使用条件下,具有106~107 Pa的杨氏模量者称为橡胶。
中文定义
Rubber is a polymer which exhibits rubber elastic properties, i.e. a material which can be stretched to several times its original length without breaking and which, on release of the stress, immediately returns to its original length.
英文定义

## Slide 8: The nature of high elasticity
High elasticity is caused by entropy change. Under the action of external force, the rubber molecular chain changes from curled state to stretched state, and the entropy decreases. When the external force is removed, the molecular chain spontaneously tends to the state of increased entropy due to thermal motion, and the molecular chain returns to curled state from stretched state, so the deformation is reversible.

## Slide 9: Rubber (Elastomers) and Rubber Elasticity
General properties of elastomers
The individual polymer chains of elastomers are held together by weak intermolecular bonding forces, which allow rapid chain slippage when a moderate pulling force is employed.
Cross-links, which are introduced during vulcanization ( 硫 化 ), permit rapid elongation of the principal sections, to a point where the chains are stretched to their elastic limit. Any additional elongation causes primary bond breakage. The cross-links, which are the boundaries for the principal sections, permit the
rubber to “remember” its original shape, that is, the original orientation of the
particular chains.
Typical applied-force-
elongation behavior of rubber
Sulphur bridges linking cis-1,4- polyisoprene
Structure of thermo-
plastic elastomers
6

## Slide 10
7

## Slide 11
8

## Slide 12: Idealized structure of a cross-linked polymer
r0
r
r0
r
A network chain segment
Network Chain
Crosslinking point
(a) (b)
relaxed, with a random coil conformation
extended, owing to an external stress
three necessary conditions for rubber elastomers:
(1) long chain polymers
(2) highly flexible
(3) crosslinked networks - moderately crosslinked

## Slide 13
橡胶态的本质？？？？？？
A simple rubber band may be stretched several hundred percent, yet on being released, it snaps back substantially to its original dimensions. By contrast, a steel wire can be stretched reversibly for only about a 1% extension. Above that level, it undergoes an irreversible deformation and then breaks. This long-range, reversible elasticity constitutes the most striking property of rubbery materials.

## Slide 14: Characteristics of rubber (elastomer) :
When the size is stable and the deformation is small, the elastic response conforms to Hooke's law, which is similar to solid.
The coefficient of thermal expansion and isothermal compression are of the same order of magnitude as liquids -- the intermolecular forces are similar to those of liquids;
The stress of deformation increases with temperature -- similar to how the pressure of a gas increases with temperature.

## Slide 15
gas
liquid
solid
Whether rubber material properties belong to solid, liquid or gas?
Certain appearance shape, size stability, small deformation in line with Hooke's law
The expansion coefficient of rubber is an order of magnitude larger than the general solid, the isothermal compression coefficient is similar to that of liquid, and the Possion Ratio is approximately equal to 0.5
The stress of deformation increases with the increase of temperature
Notes: 世界的物质状态由三种：气体，液体，和固体，而橡胶的特殊之处在于其兼有固、液、气三者的特性
固体：橡胶有一定外观形状，尺寸稳定，在小形变时符合虎克定律的应力－应变关系
液体：橡胶的膨胀系数比一般固体大一个量级，等温压缩系数与液体类似，Possion Ratio近似于0.5，即几乎是不可压缩的，与液体类似
气体：气球:在加热时，气体对球皮的压力会增加。而橡胶的拉伸长度也随温度升高而减小也正是熵弹的体现。
Analogies can be found between rubbers and gases. An increase in the chaotic state of the molecules (increase in entropy) occurs in both cases with increasing temperature. As a result, the rubber decreases in length (extension) with increasing temperature under a constant load. The same trend is indeed obtained in a compressed gas, the latter expanding (deformation=(volume)-1) when the temperature is increased. The pressure of the gas is predominantly entropically driven and so is the stress in the rubber.

## Slide 16: High Strain 弹性形变量大且是可逆的
一般铜、钢等金属的形变只有原试样的1%，而橡胶的高弹形变高达1000%
拉伸
回缩
Notes: 用图片表示
1。弹性模量小而形变量很大，而且弹性形变是可恢复的。因此把橡皮类物质的弹性形变叫做高弹性形变。一般铜、钢等的形变是原试样的1%，(若考虑严格符合虎克定律的金属，则其典型弹性形变一般小于0.2%),而橡胶的高弹性高达1000%。橡皮的弹性模量比其它固体物质小一万倍以上。——原因：熵弹entropy-driven，分子改变形状的能力.能弹-energy-driven
Metal or other highly crystalline materials exhibit Hookean elastic behaviour at strains typically less than 0.2%. Their elasticity is dominantly energy-driven.
Rubbers exhibit predominantly entropy-driven elasticity. This was discovered by Gough(1805) and later by Lord Kelvin (1857) and Joule(1859) through measurements of force and specimen length at different temperatures. They discovered the thermoelastic effects (a)that a stretched rubber sample subjected to a constant uniaxial load contracts reversibly on heating; and (b) that a rubber sample givens out heat reversibly when stretched. These observations were consistent with the view that the entropy of the rubber decreased on stretching.

## Slide 17: Low Modules The elastic modulus is small and increases with increasing temperature
橡胶高弹模量约为105N/m2
金属的弹性材料的模量可达1010~11N/m2
E= / 
Notes: 2。弹性模量小且随温度升高而增大——与金属正好相反，金属随温度升高变软(如2002年911的世贸倒塌就是因为钢筋结构在高温下模量减小，倒塌），其弹性模量随温度升高而变小。高弹模量约为105N/m2,而一般金属的弹性材料的模量可达1010~11N/m2.

## Slide 18: The modulus increases with increasing temperature
金属模量随温度升高而降低
金属
橡胶
Notes: 2。弹性模量小且随温度升高而增大——与金属正好相反，金属随温度升高变软(如2002年911的世贸倒塌就是因为钢筋结构在高温下模量减小，倒塌），其弹性模量随温度升高而变小。高弹模量约为105N/m2,而一般金属的弹性材料的模量可达1010~11N/m2.
A very illuminating experiment is to subject a rubber band to about 100% strain by hanging a dead load on to it and then heat the rubber band. The elongation of the rubber band will suddenly decrease when it is heated. This may first seen anomalous, but after reading this chapter you will understand the reason.

## Slide 19: Thermal Effect Accompanied with Strain
伸长率(%) | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800
伸长热(KJ/Kg) | 2.1 | 4.2 | 7.5 | 11.1 | 14.6 | 18.2 | 22.2 | 27.2
The relationship between rubber elongation and heat of elongation
Notes: Try it by the students.
4。形变有热效应——如果把橡胶的薄片拉长，把它贴在嘴唇或面颊上，就会感觉到橡皮在拉伸时发热，回缩时会吸热，而且拉伸时的热效应随伸长率而增加，这些性质统称为热弹效应。
舌头的敏感度为0.01C，所以是最敏感的感觉器官，可以觉察到这个温度的变化。橡皮拉伸5倍时，温度大约提高5-10度
The reversible temperature increase which occurs when a rubber band is deformed can be sensed with your lips, for instance. It is simply due to the fact that the internal energy remains relatively unchanged on deformation, i.e. dQ=-dW(When dU=0), where Q is heat and W is work. If work is performed on the system, then heat is produced, leading to an increase in temperature. The temperature increase under adiabatic conditions can be substantial. Natural rubber stretched to =5 reaches a temperature which is 5-10K higher than that prior to deformation. When the external force is removed and the specimen returns to its original, unstrained state, an equivalent temperature decrease occurs.

## Slide 20: Rubber Elasticity
vs
Energy-driven
  Energy-driven elasticity
typical of crystalline solids
entropy-driven elasticity
Entropy-driven elasticity of rubber materials
  A stretched rubber sample subjected to a constant uniaxial load contracts reversibly on heating
  A rubber sample gives out heat reversible when stretched
9

## Slide 21
橡胶弹性的本质:熵弹性

## Slide 22
6.2 Thermodynamics of Rubber Elasticity
橡胶弹性的热力学方程——本质？？
The expression form and physical significance of rubber thermodynamic equation
Thermodynamic analysis was carried out with a molecular chain network with moderate crosslinking and completely reversible deformation as the model. The rubber was a thermodynamic system and the environment was external force, temperature and pressure. The reversible deformation experiment was completed under constant temperature and pressure

## Slide 23
H
PV
U
PV
F
TS
TS
G
H = PV + U
F = U -TS
G = H –TS = U + PV -TS

## Slide 24
dQ=TdS
热力学第二定律---不可能把热量从低温物体传到高温物体而不产生其他影响。
假设拉伸过程为等温可逆，根据热力学第二定律：
膨胀功+拉伸功
dW =PdV-fdl
单轴拉伸过程体系对外界所作的功为
dU =TdS-PdV+fdl
橡胶在等温拉伸中体积不变， 即dV=0
dU =TdS+fdl（等温等容）
Notes: 假设过程是可逆的，由热力学第二定律可得dQ=TdS. Second law of thermodynamics， 法国物理学家 Nicloas Leonard Sadi Carnot (1796~1832)在发明永动机时就注意到的问题，但他没能提出来，真正的工作是由德国物理学家Rudolph Clausius (1822~1888)完成的——克劳修斯表述：不可能把热量从低温物体传到高温物体而不产生其他影响。——即热量的变化必定伴随着熵变，即我们看到的这个例子。
不可能从单一热源吸取热量，使之完全变为有用的功而不产生其他影响。或第二类永动机是不可能造成的。第二类永动机是能从单一热源吸取热量并使之完全变为有用的功而不产生其他影响的机器。虽然，它并不违反第一定律。
Third law of thermodynamics是研究当温度趣于绝对零度时物质性质的热力学定律，即用任何方法都不能使系统达到绝对零度

## Slide 25
H=U+PV
dU =TdS+fdl（isothermal-isobaric）
内能变化
熵变化

## Slide 26
等温等容条件下：
物理意义：外力作用在橡胶上，一方面使橡胶的内能随伸长变化，另一方面使橡胶的熵随伸长变化。
橡皮的在恒温恒压下的可逆形变，其分子间距离不变，即分子间相互作用不变，只考虑分子构象的改变对内能和熵的改变！！
？？内能和熵各占多少？？

## Slide 27
变换
吉布斯自由能 G=H-TS
=U+PV-TS
微小变化： dG=dU+PdV+VdP-TdS-SdT
(dU=TdS-PdV+fdl)
=VdP-SdT+fdl
不可测！

## Slide 28
Physical significance: when the length and volume of the sample are unchanged,
Variation of specimen tension f with temperature

## Slide 29: f-T Curve of tensile force against temperature
各直线外推到T= 0 时，几乎都通过坐标的原点
绝对零度T=0K
T
f
形变量减小
(dU／dl)T,V≈0
伸长率小于10％
Notes: 实验时，将橡皮在等温下拉伸到一定长度l，然后测量不同温度下的张力f。因为上式是按平衡态热力学处理得到的，实验改变温度时必须等待足够的长的时间，使张力达到平衡为止。
问题：表明什么？表示在橡皮拉伸过程中，内能的变化几乎为零。所以外力仅仅使熵变。

## Slide 30: 外力作用引起熵变：
The system entropy of rubber decreases under the action of tensile stress, and the spontaneous process of entropy increase after the release of external force restores the original state
(dU／dl)T,V≈0
Notes: 把（18）代入（17）式得（19）
金属弹性是能弹性，熵变为零
拉伸时，f>0,dl>0, 所以dS<0; 回弹时，f=0，dS>0

## Slide 31
fdl =-TdS= - dQ
stretch dl>0, dS<0
dQ<0 Tensile heat release
rebound dl<0, dS>0
dQ>0 Retraction endothermic
dU=0
dV=0
dU =TdS-PdV+fdl
dQ=TdS
Explain that rubber exotherms heat when stretched and endotherms when retracted
Under isothermal and isovolumic conditions:
Notes: 用（18）和（5）代入（4）得（20），再考虑热能的定义（3），即第二热力学定律，得（21）式。
定义dQ是拉伸时需要的热量，所以为负时是放热，为正时是吸热
讨论：
橡胶在绝热拉伸过程中 放 热，橡胶的模量随温度的升高而 升高 。

## Slide 32
6.3 Statistical Thermodynamics of Rubber Elasticity
橡胶弹性的统计热力学
Chapter 6

## Slide 33: 仿射形变
网络中的各交联点被固定在平衡位置上，当橡胶形变时，这些交联点将以相同的比率变形。
Notes: 第五为仿射形变假设
所以先考虑仿射形变。——其本质意义是把微观形变看作与宏观形变完全相似。即宏观x方向伸长x倍，微观网也在x方向伸长x倍。
——仿射形变 是从仿射几何 Affine geometry学开始研究的,研究的是投影的性质，图为平行投影示意图

## Slide 35: The statistical mechanics of rubber elasticity
Affine network (仿射网络)
The chain segments between crosslinks can be represented by Gaussian statistics of unperturbed chains.
The network consists of N-chains per unit volume. The entropy of the network is the sum of the entropies of the individual chains.
All different conformational states have the same energy.
The deformation on the molecular level is the same as that on the macroscopic level, i.e. deformation is affine.
The unstressed net work is isotropic.
The volume remains constant during deformation.
11

## Slide 36: The statistical mechanics of rubber elasticity
dxdydz






 
0
The distribution of the end-to-end distance vector
3 / 2
0 
2 r 2
3(x2  y2  z2 ) 

exp 
3
P(x, y, z)dxdydz   
 2 r 2
0
3
r2
2 r2
 3


 3(x2  y2  z2 ) 

S  k ln P(x, y, z)  k  ln 
  
 2
 
 2


0  


0
2 r 2
3r 2
S  C  k
Deformation of a random chain from unstressed state r0 to stressed state r
x  1x0 y  2 y0 z  3 z0




0
 0 0 0 
0
2 r 2
 3(x2  y2  z2 ) 
S  C  k






0
2 2
2 2
1 0 2 0 3 0 
2 r 2
S  C  k
  z )
3( x  2 y2






0
2
0 
3
0
2
1
2 r 2
1)z
1)x2
S  S  S0  3k
 (2
 (2 1) y2
2 0
(







0
2 
2 2
 1 1 1 
2 2
2
1  0 2  0 3
1
2 r 2
 S  3k
S
n
n
n
n
N 
y  ( 1) z0 
 ( 1) x  ( 1)
The entropy
12

## Slide 37
The statistical mechanics of rubber elasticity




0
1 0 2 0 3 0 
0
2 r 2
S  S  S  3k
 (2 1)x2  (2 1) y2  (2 1)z2 







 
0
2 
2 2
1 1 1

2 2
0 2 0 3
2
1

1
2 r 2
S  3k
n
n
n
n
SN 
1) y  ( 1) z0 
1) x  (
 (
n
n
n
x  y  z
1
1
2 2
2
 0  0  0
1
 
n
n
n
n
z  r
x
1
2
1
2
0  0
y
1
2
0

1
2
0
2
2
2
2
2
0
1
1
3
3
n
n
n
n
N r
x  y  z 
r 
 0  0  0
1 1
 0
1

2
2
2
1
2
3
1
2
N
Nk 
S  
 
   3

2
2
2
1
2
3
1
2
N
A  T S
 NkT 
 
   3
13

## Slide 38: The equations of state of rubber elasticity
t
       
1 2 3

1
t 
0
l
l
 
  
f   (A) 
  (A) 
   
l

 l 


T ,V T ,V  T ,V
2
2
0
1
NkT
l


 
  1
2   l




f 
NkT    3

 




  2
  




 l  l0 
 
0
0
2
1
A
NkT
l
A / 






 


  
0 

 
For uniaxial stress,
(volume remains constant)
,
123  1,
2
t

 1,
,
2
0
1
NkT
V


 

   
 
True stress
“Modulus” increase in a linear manner with increasing temperature. This is a typical entropy-elastic.
True stress
  f /
A0: cross section area of the unstrained rubber
V0: the volume of the rub14ber

## Slide 39: The equations of state of rubber elasticity
c
a
a
c
N
V
V
M V M

M
N  nM N  1 
 m  1 
 
a     0 
 N 
0  0  c   0  c 




 

 
2
c
M
RT  1 
Rubber with high crosslinking
density, i.e. low Mc, behave stiff
2
c
M

   RT    1 
 
 
True stress (真应力)
Nominal stress (习用应力)
2
2
0
1
NkT
l


 
  1 2   l
 


f 
NkT    3

 




  2
  





l  l0 
0
A
  f
solids
0
c
M
l
 0
  3  RT  1
   E  E l  l0  E  1
Small strain limit: 1
c
E  3  RT
Note: =l/l0=1+
1M5

## Slide 40
Gel Swelling
Isotropic swelling of a network polymer
1/ 3
1 2
1,el
c
M
 RT
V 
 

2
2
2 2
2
1,mix

2  x  2
  RT  ln(1  )  1 1   
2 
 


 RT ln(1  )    
* * *
*1/ 3
1
2
2
2
2
c
M
V

ln(1  )     
 0
0 2
1 2 3 V
V

    V    1
3
1 2 3 V
        
2
1/ 3
  

 
0
2
el
c
2M
3 RTV

2 / 3
Swelling of rubbers in solvents F
 1 NkT 3 2  3 
1
(2: volume fraction of polymer component in swollen gel)
Flory-Huggins solution theory:

At swelling equilibrium
1  1,el  1,m  0
2
V0
 
V0  n1V1
1 1
2 1
2
F F F 
1 
m el 2  0
n n
 n
(Flory-Rehner equation)
16

## Slide 41: Deviations from classical statistical theories
Crosslinking of a polymer with finite MW indicating the formation of loose chain ends.
“Chain defects” in network: (a) permanent physical crosslink; (b) temporary physical crosslink; (c) intramolecular crosslink.
=l/l0
(a) (b) (c)
Segment vectors do not follow Gaussian statistics when rubbers are highly stretched.
At high extension ratio, crystallization may occur in rubbers.
17

## Slide 42: Equation of State
状态方程
dW  fdl
0
2
l
⎠
⎜ ⎟
⎝
⎠T ,V
⎜ dl ⎟
⎝
⎠T ,V
⎝
⎠T ,V
⎜ dl ⎟
⎝
f  ⎛ dW ⎞  ⎛ dW ⎞

 NkT ⎛   1 ⎞  1
 ⎛ d ⎞
⎜ d ⎟
⎠
⎜ ⎟
⎝
2
0 0
0

 NkT ⎛   1 ⎞
A A l
  f
⎠
⎜ ⎟
⎝
2

c
M
  RT ⎛   1 ⎞
⎠
⎜ ⎟
⎝
2
1

  N kT ⎛   1 ⎞
状态方程
单位体积试 样的网链数
试样的密度
网链平均分子量
⎝
⎜ 2 ⎟
1
 ⎠
  n RT ⎛   1 ⎞
单位体积试样 的网链摩尔数

## Slide 43: Deviations from classical statistical theories
Crosslinking of a polymer with finite MW indicating the formation of loose chain ends.
“Chain defects” in network: (a) permanent physical crosslink; (b) temporary physical crosslink; (c) intramolecular crosslink.
=l/l0
(a) (b) (c)
Segment vectors do not follow Gaussian statistics when rubbers are highly stretched.
At high extension ratio, crystallization may occur in rubbers.
17

## Slide 44
An Example of Rubber Elasticity Calculations

## Slide 45
⎠
⎜ ⎟
⎝
2
1

  n RT ⎛   1 ⎞
例题 2：Suppose an elastomer of 0.1cm0.1cm10cm is stretched to 25cm length at 35℃, a stress of 2107dynes/cm2 being required. What is the concentration of active network chain segments?
1
RT  1 2 
n 
 = L/L0 = 25/10 = 2.5
n1 = 3.34104 mol/cm3
2 107 dynes/cm2
n1  8.31107 (dynescm/molK)  308K  2.5 1 2.52 
N1 = 21020 /cm3

## Slide 47: 课堂测
1. 如果加一重物于交联橡皮筋，保持恒定的张力，当加热该橡胶时，重物位置如何变化？（ ）
A. 升高 B 降低 C 不变
2. 有关橡胶高弹性的描述正确的是（ ）？
A 弹性模量低 B 形变量较小 C 能弹性 D 压缩时放热
3. 产生高弹性的分子结构特征是 （ ）？
A 分子链具有一定柔性
B 分子之间具有强烈的相互作用
C 分子链之间化学键连接 D 常温下能够结晶
E 相对分子质量足够大
4. elastic deformation （ ) entropy elasticity（ ) one-way drawing （ ) elasticelongation （ ) Poisson’s ratio （ )
思考题: 在橡胶下悬一砝码，保持外界不变，升温时会发生什么现象？

## Slide 48: 小结
Concepts: Stress, strain, elastic modulus, thermoplastic elastomer
Characteristics and essence of rubber elasticity
The relationship between high elasticity and molecular chain structure
Thermodynamic analysis of rubber elasticity and its significance
Understand the equation of state of elasticity of crosslinked rubber